Investigating Bond Characteristics and Structural Efficiency of High-Density Polyurethane Foam Infill in Aluminum and Light Gauge Steel Tubes

Padmaja Gokarajua*, V.V.V.S. Murtyb, N.V. Ramana Raoc

a*Vice President -Designs, R&D, Kirby Building Systems and Structures India Pvt., Ltd., Hyd.

bDean (R&D), SIET, Ibrahimpatnam, Ranga Reddy District, Telangana, India

cDirector, National Institute of Technology, Raipur, Chhattisgarh, India
*gpadmaja@kirby-india.com

Abstract. Global infrastructure development demands sustainable, cost-effective construction solutions with high strength-to-weight ratios. Recent studies show that composite systems using lightweight aluminum and light gauge (LG) steel tubes filled with high-density polyurethane (PU) foam significantly improve compressive and flexural strength due to their composite action and bonding effects. This study investigates the bond characteristics of high-density PU foam-filled aluminum and LG steel tubes, utilizing experimental and numerical evaluations. The findings reveal that confined PU foam exhibits significantly enhanced strength compared to unconfined PU foam, due to triaxial confinement and cell structure rearrangement. The bond between aluminum and high-density PU foam demonstrates reasonable accuracy compared to the steel-concrete bond. Although high-density PU foam-filled steel square tubes show slightly lower compatibility than aluminum circular tubes, both configurations offer substantial improvements in bond performance, validating their flexural and compressive strength enhancements. Further research on LG steel square tubes should be carried out by introducing ribs for improving bond behaviour. These composite systems are suitable for applications in structural components, including bracings, solar panel supports, and lightweight shelters. However, the study highlights the potential of using high-density PU foam as an effective infill material in lightweight structural applications, contributing to the advancement of sustainable construction practices

Keywords: Sustainable Construction; Strength to-weight ratio; Economical solution; Composite system; High-density polyurethane foam; Aluminum tubes; Galvanized steel tubes

# Introduction

The increasing global emphasis on infrastructure development necessitates sustainable and cost-effective solutions within the construction industry. Optimization of geometry and material properties plays a pivotal role in meeting these demands. Structural elements with high strength-to-weight ratios are particularly valued for their ability to offer superior strength while remaining economical. This ratio is extensively explored in composite systems that leverage diverse material properties to enhance overall performance. Such optimization results in enhanced strength-to-weight ratios, which are essential for meeting modern construction requirements. Hollow tubes are commonly employed due to their higher stiffness and mitigate torsional effects. However, their thin-walled sections make them susceptible to local buckling. This challenge can be effectively resolved using sustainable infill materials.

## Materials

Aluminum, galvanized LG steel, and High-density polyurethane (PU) foam are chosen for this study based on their distinct properties and established performance across diverse engineering applications [1,2]. Aluminum and LG steel are highly valued for their lightweight nature, corrosion resistance, thermal and electrical conductivity, and sustainability. They are widely utilized in construction and various other industries. Notably, Padmaja [3] highlights aluminum tubes filled with high-density PU foam as the sustainable and economical solution in composite systems considering their significant ratio of strength to weight.

High-density Polyurethane (PU) foam is widely utilized in engineering due to its cost-effectiveness, versatility, and exceptional properties such as energy absorption, impact resistance, and insulation. Zhang et al. [4] observed that the rise in foam tube’s overall energy absorption is attributed to interactions at the contact surface. Temperature, material orientation, density, and loading rate all affect how PU foam’s dynamic compression behaviour [5]. The studies also demonstrated that the binding properties of PU foam with metal surfaces are adequate, making it suitable for aerospace and automotive applications. Research has consistently shown that higher foam densities enhance PU foam performance under dynamic loading [6-7]. This study employs high-density PU foam (150 kg/m³) as an infill material for cold-formed LG steel square tubes and circular aluminium tubes, leveraging its superior performance attributes.

## Bond strength

Further literature investigation has focused on evaluating the bond strength of composite elements. Virdi et al. [8] evaluated the strength of the bond between the concrete core and the steel tube by testing concrete-filled steel tubes. Their study explored various parameters such as the ratios of tube diameter to thickness, length to diameter, and compressive strength of concrete. They concluded that bond resistance is primarily influenced by the interlocking mechanism between concrete and the steel surface, encompassing both micro locking from surface roughness and macro locking from manufacturing tolerances. Song et al. [9] carried out pull-out tests at various temperatures (20 to 800°C) on steel tubes filled with concrete. Their findings indicated that cross-sectional shape, concrete type, and steel type significantly influence bond behavior, with carbon steel demonstrating higher bond strengths than stainless steel. In their investigation of the effects of bonded and unbonded infill materials on the bond strength of aluminum foam-filled structures, Santosa et al. [10] found that bonded foam had a 60% higher mean crushing force because of the increased adhesion between the tube wall and the core infill. Hanssen et al. [11, 12] examined the crushing response of aluminum foam-filled extrusions, focusing on the impact of bonded foam in suppressing progressive folds and global rupture. Their research highlighted a significant decrease in the elasticity modulus with bonded foam configurations. The above post-study showcases the influence of bond behavior in enhancing the capacity of composite-filled tubes.

## Composite High-Density PU Foam-Filled Tubes

The galvanized LG steel and aluminum tubes are increasingly popular in modern construction due to their favorable strength-to-weight ratios and ease of fabrication. When combined with sustainable polyurethane (PU) foam, these materials exhibit enhanced composite behavior [1-3]. High-density PU foam offers excellent energy absorption and confinement, stabilizing the interface between the steel or aluminum and the foam. This confinement helps to control geometric failures related to local buckling and allows the material to yield until the plastic state, enhancing the load-carrying capacity. Research has demonstrated that using high-density PU foam infill can significantly improve the compressive (refer to Table 1) and flexural strength of these composite sections, attributing their bonding effects and making them highly efficient for structural applications.

Table 1. Compressive strength enhancements of High-Density PU foam-filled tubes [1]

| D/t | L/D | Mean Compressive Force (kN) |  |  |  | Enhancement (%) from (foam + tube) to (foam filled tube) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | PU Foam | Tube | PU Foam + Tube | PU Foam Filled Tube |  |
| High-density PU foam-filled aluminum circular tubes. |  |  |  |  |  |  |
| 40.20 | 3.32 | 2.58 | 28.27 | 30.85 | 46.77 | 51.60 |
| 30.15 | 3.32 | 2.58 | 39.88 | 42.46 | 49.10 | 15.64 |
| High-density PU foam-filled LG steel square tubes. |  |  |  |  |  |  |
| 125.00 | 2.00 | 2.58 | 19.29 | 21.87 | 32.80 | 49.98 |
| 125.00 | 3.00 | 2.58 | 18.67 | 21.25 | 33.53 | 57.79 |
| 125.00 | 4.00 | 2.58 | 23.28 | 25.86 | 45.87 | 77.38 |
| 100.00 | 2.00 | 2.58 | 29.92 | 32.49 | 44.05 | 35.58 |
| 100.00 | 3.00 | 2.58 | 34.60 | 37.18 | 48.58 | 30.66 |
| 100.00 | 4.00 | 2.58 | 35.00 | 37.58 | 49.04 | 30.49 |
| 83.33 | 2.00 | 2.58 | 36.37 | 38.95 | 54.51 | 39.95 |
| 83.33 | 3.00 | 2.58 | 39.50 | 42.08 | 61.45 | 46.03 |
| 83.33 | 4.00 | 2.58 | 39.88 | 42.46 | 71.68 | 68.82 |

Despite the promising results from previous studies, which highlight significant strength enhancements due to the composite action of high-density PU foam-filled tubes over the combined load-carrying capacities of empty tubes and foam alone, further investigation is carried out into the bonding effects between high-density PU foam and LG steel as well as aluminum. The bond strength significantly affects energy absorption, delays local buckling, and enhances the overall structural performance of composite members. Thus, the study aims to provide a comprehensive insight into the bond characteristics between high-density PU foam and metal tubes and their impact on the structural behavior of composite sections. This research signifies the potential of high-density polyurethane (PU) foam as a sustainable infill material for aluminum and light gauge (LG) steel tubes by demonstrating how triaxial confinement and foam-to-metal bonding enhance both compressive and flexural strengths. The study validates the composite behavior of confined PU foam within tubes, contributing to sustainable construction practices for lightweight infrastructure.

# Test Specimens

## Material Properties

The mechanical properties of the materials utilized in this study, namely aluminum, galvanized LG steel, and polyurethane (PU) foam, were thoroughly assessed to ensure accurate characterization. The selection of material grades adhered strictly to industry standards and guidelines. Aluminum samples, following the ASTM A6061-T6 specification, are 3.2 mm thick and underwent tensile coupon testing in a 60-ton capacity Universal Testing Machine (UTM) at 78.8°F according to The Aluminum Association Structural Design standards.

High-strength cold-formed steel, produced through rolling, pressing, stamping, and bending at room temperature, conforms to ASTM A570 specifications. Galvanized Cold Rolled Steel, meeting ASTM A 653/653M-07 [13] Grade 340 Class 1 standards, was also coupon tested for mechanical properties using ASTM A370 procedures [14].

PU foam, selected for its density of 150 kg/m³ and excellent energy absorption capabilities, underwent mechanical testing. This included uniaxial compression tests on foam cubes (refer Sec 3.1) and tensile coupon test (refer Fig. 1) according to ASTM D1621 [15] and ASTM D3574 [16], respectively. The mechanical properties of the 150 kg/m³ PU foam are comparable to M14 grade concrete. Detailed material properties are summarized in Table 2.

Fig. 1. (a) Tensile Coupon Test Setup for high-density PU Foam (density: 150 kg/m³), and (b) Axial Tension Stress vs. Strain Behaviour.

Table 2. Material Properties

| Material | Density | Yield Strength | Ultimate Strength | Elasticity Modulus | Poisson’s ratio | Elongation |
| --- | --- | --- | --- | --- | --- | --- |
|  | (kg/m3) | (MPa) | (MPa) | (MPa) |  | (%) |
| Aluminium | 2700 | 261.62 | 274.55 | 65404 | 0.33 | 7.6 |
| GI Steel | 7850 | 345 | 450 | 200000 | 0.3 | 12 |
| PU Foam (T) | 150 | 1.587 | 1.80 | 158.5 | 0.33 | 8 |
| PU Foam (C) | 150 | 5.2 | 14.03 | 226 | 0.33 | NA |

Note. T: Tension, C: Compression.

## Geometric properties

Specimen selection for experimental evaluation considered practical application ratios to ensure relevance to real-world scenarios. Hollow circular aluminum tubes were machined to achieve diameter-to-thickness ratios of 30.15 and 40.20 (longitudinal aspect ratio), with a length-to-diameter ratio of 3.32 (cross-sectional aspect ratio). Galvanized cold-rolled steel coils were formed into 100 mm side square tubes with thicknesses of 0.8 mm, 1.0 mm, and 1.2 mm. These tubes, 200 mm in length, were fabricated using the press braking process, with corners secured by rivets and tack welding at 50 mm intervals. Details of the aluminum and light gauge steel specimens prepared for experimental tests are summarized in Table 3.

Table 3. Geometric Properties

| Specimen | Length | Thickness | Diameter/Width | L/(D/B) | (D/B)/t | No. |
| --- | --- | --- | --- | --- | --- | --- |
|  | (L mm) | (t mm) | (D/B mm) |  |  |  |
| FFAC1 | 200 | 2.0 | 60.3 | 3.32 | 30.15 | 4 |
| FFAC2 | 200 | 1.5 | 60.3 | 3.32 | 40.20 | 4 |
| FFSS1 | 200 | 0.8 | 100.0 | 2.00 | 125.00 | 3 |
| FFSS2 | 200 | 1.0 | 100.0 | 2.00 | 100.00 | 3 |
| FFSS3 | 200 | 1.2 | 100.0 | 2.00 | 83.33 | 3 |

FFAC: High-density PU Foam Filled Aluminum Circular Tube, FFSS: High-density PU Foam Filled Steel Square Tube.

# Experimental Investigation

The experimental investigation utilized the push-in test procedure to assess the bond capacity of the specimens. The experimental setup, depicted in Fig. 2, involved hollow test specimens measuring 200 mm in length, filled with high-density PU foam up to 190 mm from the bottom. A compressive load was applied exclusively on the foam at a rate of 50 mm/min using a 100 kN Universal Testing Machine (UTM).

Fig. 2. (a) Experimental Setup - Testing of high-density PU foam filled (b) aluminum circular tubes and (c) galvanized steel square tubes.

The crushing strength of high-density PU foam confined within hollow elements, including high-density PU foam-filled aluminum circular tubes and light gauge steel square tubes, was compared with that of unconfined foam (PU foam alone). This approach facilitated the evaluation of the bond strength between the high-density PU foam and the hollow tubes, with load versus slip data used to measure the contact interface bond strength.

## Behavior of unconfined high-density PU foam

The unconfined PU foam (150 kg/m3) of 50 mm side cubes was subjected to uniaxial compression to investigate behavior in terms of stress versus strain response illustrated in Fig. 3.

Fig. 3. (a) Compression testing of unconfined high-density PU foam and (b) Stress-strain behavior of unconfined high-density PU foam.

Polyurethane foam exhibits distinct regions in its stress-strain behavior under compression:

Linear Elastic Region (AB): At smaller strains, the high-density PU foam behaves linearly elastic, with the slope of this region equal to Young's modulus. The obtained Young's Modulus (AB) is 226 MPa.

Plateau Region (BC): Following the linear elastic region, the stress nearly remains unchanged in the plateau region, indicating energy absorption capacity.

Densification Region (CD): Finally, in the densification region, stress increases rapidly with further strain due to the collapse of the foam cells.

The compressive stress observed at 10% displacement was 5.2 MPa. The ultimate compressive stress achieved was 14 MPa, which is comparable to the strength of M14-grade concrete. However, the split tensile strength for M14 concrete is 1.5 MPa, whereas for PU foam, it is 1.6 MPa.

## Behavior of confined high-density PU foam within the aluminum circular tube

Push-in tests were conducted to investigate the behavior of confined PU foam within aluminum circular tubes concerning bonding effects. The results, presented in Fig. 4(a) and 4(b), illustrate the load-slip and stress-strain response, respectively. The responses for both specimens (D/t of 40.2 and 30.15) are almost aligned together with a slight variation, indicating circular aluminum tube wall thickness has a slight influence on bond performance.

Fig. 4(a). Load-slip behavior of confined PU foam within the aluminum circular tube.

Fig. 4(b). Stress-strain behavior of confined PU foam within the aluminum circular tube.

Upon observation, the confined high-density PU foam exhibited behavior similar to that of the unconfined foam, with key differences. It showed an enhanced linear elastic region (AB’) extending to greater strains, a shorter plateau region (B’C’) for energy absorption, and a slight densification region (C’D’) leading to failure. Key observations are as follows:

- In unconfined conditions, a compressive stress of 5.2 MPa was observed at 15% slip (7.5 mm). When confined within aluminum, this stress significantly increased to 13.8 MPa at the same 15% slip (28.5 mm).

The composite action between the high-density PU foam and the aluminum tube resulted in a 2.65 (13.8/5.2) times improvement in compressive stress compared to the unconfined state.

The Elastic Modulus of PU foam confined within the aluminum envelope was calculated to be 6900 MPa, corresponding to the slope of the linear elastic region.

However, in the densification region at D point, the high-density PU foam confined within an aluminum circular tube also provides a stress of 13.8 MPa along with unconfined high-density PU foam demonstrating comparable characteristics with M14 concrete.

## Behavior of confined high-density PU foam within LG steel square tube

The load versus slip response and computed stress-strain behavior for confined high-density PU foam within LG steel square tubes are represented in Fig. 5(a) and 5(b), respectively. For LG steel square tubes, the wall thickness shows significant variation in bond performance beyond the elastic region, attributing to inadequate interactions between LG tube and foam at corners of the square section.

Fig. 5(a). Load-slip behavior of confined high-density PU foam within LG steel square tube.

Fig. 5(b). Stress-strain behavior of confined high-density PU foam within LG steel square tube.

The behavior is similar to that observed for confined PU foam within aluminum circular tubes, though with a slightly reduced elastic region. The measurements were carried out using the same methodology, and the key findings are as follows:

- Under confinement with steel, a compressive stress of 6.3 MPa was observed at 10% slip. This represented a 1.21 (6.3/5.2) times improvement in compressive stress compared to the unconfined state.

The Elastic Modulus of high-density PU foam confined within the steel envelope was calculated to be 3150 MPa.

These observations underscore the effectiveness of confinement in enhancing the compressive properties of high-density PU foam, though the degree of enhancement varies with the type of material used for the tube.

## Failure mode

The failure mode following the plateau region and slight densification illustrate lateral buckling and bulging behavior. The confined high-density PU foam, under compressive stresses, experiences lateral tensile strains, leading to lateral expansion. This failure behavior is depicted in Fig. 6.

Fig. 6. High-density PU foam-filled tube behavior at (a) load initiation and (b) failure stage.

# Numerical Investigation

Finite element analysis (FEA) was conducted using the software ABAQUS 6.14-3. Shell elements were used to model the tubes, while solid elements were used to represent the foam. Specifically, a 2D S4R shell element, where “R” stands for hourglass control within the element, was used to record all six degrees of freedom.

The foam was modelled using a C3D8R element type, totaling 693,000 elements. Penalty contact exhibiting tangential behaviour was utilized to model the bonding interface between the foam and the tube. Furthermore, a frictionless tie connection was made between the foam, tube, and stiff plates. A dynamic explicit non-linear analysis was performed with the loading rate of 100 mm/0.05 sec, and loading continued until the foam was crushed up to 60% of its length. The stages of the finite element analysis are depicted in Fig. 7.

Fig. 7. Finite Element Model of (a) unconfined high-density PU Foam and (b) (i) high-density PU Foam-Filled Tube for Bond Test, (ii) Before and (iii) After Compression at 30%.

To validate the experimental findings, the results from the FEA were compared with experimental data, specifically focusing on the load versus slip behavior. Comparative plots for unconfined PU foam and PU foam confined within aluminum tubes are illustrated in Figs. 8(a) and 8(b), respectively.

Upon observing the above comparative study, it is noted that the FEA results exhibit a slight underestimation for unconfined foam and a slight overestimation for confined high-density PU foam within aluminum tubes compared to experimental findings. These slight variations can be attributed to practical imperfections and residual stresses. Nevertheless, the FEA results demonstrate reasonable accuracy in capturing the structural behavior consistent with experimental observations.

Fig. 8. Comparison of FEA and Experimental Results for (a) Load-Displacement Behaviour of Unconfined high-density PU Foam and (b) Load-Slip Behaviour of Confined high-density PU Foam within aluminum tubes.

# Results and Discussions

The findings from the experimental and numerical investigations are interpreted and discussed in the following points:

- The stress ratios between confined and unconfined conditions, greater than 1, indicate enhanced capacity due to triaxial confinement and resisting tangential frictional stresses at the interface. The bond between aluminum and high-density PU foam demonstrates superior performance compared to steel and high-density PU foam, primarily due to their similar Poisson ratios which mitigate varying bulging effects. Consequently, the improvement in stiffness due to infill is approximately one-third less in steel tubes compared to aluminum tubes, particularly when both are in circular configurations.

In comparison to well-established concrete-filled steel tubes, which typically exhibit a confined to unconfined stress ratio of 2 [17], the aluminum- high-density PU foam bond shows a higher ratio of 2.6, indicating superior interface connectivity than steel-concrete bonds. However, the galvanized steel-high-density PU foam bond exhibits a lower ratio of 1.25, indicating less compatibility.

Evaluating elastic modulus (E) compatibility ratios (Eenvelope / Einfill), aluminum-high-density PU foam demonstrates a ratio of 9.48. This ratio is slightly lower than the steel-concrete ratio of 10.33 but remains favorable for structural applications.

The coefficient of thermal expansion for aluminum is 24 × 10⁻⁶ /°C, for steel is 13 × 10⁻⁶ /°C, and for concrete is 10 × 10⁻⁶ /°C. Polyurethane high-density (greater than 100 kg/m³) in-situ rigid foam has a coefficient of thermal expansion ranging from 24 to 57.6 × 10⁻⁶ /°C. Consequently, high-density polyurethane foam is more compatible with aluminum and nearly compatible with steel in terms of thermal expansion.

The composite behavior of high-density PU foam aligns with the investigations by Menges and Knipschild [18], indicating that its strength is derived from the rearrangement of the cell structure under loading, resembling a space frame.

Overall, the high-density PU foam infillment for aluminum circular tubes demonstrates higher compatibility than for LG square tubes. However, both tubes offer significant enhancements in compressive, flexural, and bond performance, making them suitable for lightweight to moderate structural applications.

# Conclusions

The following conclusions can be stated as a result of this study,

- The high-density PU foam-filled tubes exhibit a higher axial load-carrying capacity compared to the combined capacities of the foam alone and the empty tube, indicating robust composite action facilitated by the tube wall and high-density PU foam bond.

High-density PU foam exhibits a much higher short-term compressive strength under confinement than concrete because of its triaxial confinement without micro-cracking, highlighting its strong link with the aluminum tube wall.

Circular aluminum tubes show superior bond effects over square steel tubes, attributed to resonating mechanical properties with high-density PU foam, notably Poisson's ratio, which mitigates bulging effects.

High-density PU foam-filled steel square tubes also demonstrate notable structural performance improvements, albeit with slightly less compatibility.

The results of finite element analysis match experimental data fairly well, indicating that it may be a more affordable option than conducting extensive experimental testing.

In conclusion, the effective bond performance of high-density PU foam-filled tubes validates previous studies’ findings on enhanced compression and flexural capacities [1, 2]. These lightweight tubes, combined with on-site foam injection for enhanced load-carrying capabilities, are particularly suited for dynamic environments such as those encountered by the Indian armed forces. Due to their efficient bonding and composite behavior, they also find applications in structural components like bracings, solar panel supports, and lightweight shelters. Further research on LG square tubes, such as introducing the ribs to improve their bond behavior, is recommended. Nevertheless, this study underscores the advantages of composite tubes filled with high-density PU foam. The insights gained contribute significantly to advancing lightweight, high-strength structural applications, enhancing structural resilience and operational effectiveness.

# References

Padmaja, M., Murty, V. V. V. S., & Rao, N. R. (2021). Quasi-static axial compression of empty and PU foam-filled circular aluminum and light gauge square steel tubes. Materials Today: Proceedings, 43, 2342-2347. Doi: 10.1016/j.matpr.2021.01.680

Mantena, P., Murty, V. V. V. S., & Rao, N. R. (2022). Flexural strength of composite high-density polyurethane foam-filled light gauge square steel tubes. Materials Today: Proceedings, 51, 2403-2410. Doi: 10.1016/j.matpr.2021.11.591

Padmaja, M., Murty, V. V. V. S., & Ramana Rao, N. V. (2019). Comparative structural performance of composite filled tubes. International Journal for Computational Methods in Engineering Science and Mechanics, 20(6), 477-486. Doi:10.1080/15502287.2018.1534160

Zhang, C. J., Feng, Y., & Zhang, X. B. (2010). Mechanical properties and energy absorption properties of aluminum foam-filled square tubes. Transactions of Nonferrous Metals Society of China, 20, 1380-1386. Doi: 10.1016/S1003-6326(09)60308-3

Linul, E., Marsavina, L., Apostol, D. A., Constantinescu, D., & Sadowski, T. (2012). Effect of density, loading rate, material orientation and temperature on dynamic compression behaviour of rigid polyurethane foams. In Proceedings of the 10th International Conference on Foam Materials & Technology (CD ROM), Barcelona.

Saint-Michel, F., Chazeau, L., Cavaille, J. Y., & Chabert, E. (2006). Mechanical properties of high-density polyurethane foams: I. Effect of the density. Composites Science and Technology, 66, 2700-2708. Doi: 10.1016/j.compscitech.2006.03.009

Onsalung, N., Thinvongpituk, C., & Painthong, K. (2010). The influence of foam density on specific energy absorption of rectangular steel tubes. Energy Research Journal, 1(2), 135-140.

Virdi, et al. (1980). Bond strength in concrete-filled steel tubes. IABSE Proceedings P-33/80, 4.

Tao, Z., Song, T. Y., Uy, B., & Han, L. H. (2016). Bond behavior in concrete-filled steel tubes. Journal of Constructional Steel Research, 120, 81-93. Doi: 10.1016/j.jcsr.2015.12.030

Santosa, S., & Wierzbicki, T. (1999). Effect of an ultralight metal filler on the bending collapse behaviour of thin-walled prismatic columns. International Journal of Mechanical Sciences, 41, 995-1019. Doi: 10.1016/S0020-7403(98)00066-6

Hanssen, A. G., Hopperstad, O. S., & Langseth, M. (2000). Bending of square aluminium extrusions with aluminium foam filler. Acta Mechanica, 142, 13-31. Doi: 10.1007/BF01190010.

Hanssen, A. G., Langseth, M., & Hopperstad, O. S. (2002). Crash behaviour of foam-based components: Validation of numerical simulations. Advanced Engineering Materials, 4(10), 771-776. Doi: 10.1002/1527-2648(20021014)4:10<771: AID-ADEM771>3.0.CO;2-Y

American Society for Testing and Materials. (2011). ASTM A653: Standard specification for steel sheet, zinc-coated (galvanized) or zinc-iron alloy-coated (galvannealed) by the hot-dip process. West Conshohocken.

American Society for Testing and Materials. (2016). ASTM A370-2016: Standard test methods and definitions for mechanical testing of steel products.

American Society for Testing and Materials. (2023). ASTM D1621: Standard test method for compressive properties of rigid cellular plastics.

American Society for Testing and Materials. (2017). ASTM D3574-2017: Standard test methods for flexible cellular materials.

Murty, V. V. V. S. (1993). Strength & behavior of light gauge steel-concrete composite members and their joints (Doctoral dissertation). Indian Institute of Technology, Kharagpur.

Menges, G., & Knipschild, F. (1975). Estimation of mechanical properties for rigid polyurethane foams. Polymer Engineering & Science, 15(8), 623-627. Doi: 10.1002/pen.760150810